WO3196 First measurements
Date: 2019 12 31 and 2020 06 01
Measured with coax cables and sourcemeter

---
Configuration
- Wire bonded to the “top row” of Hall bars, i.e. the ones with the largest amount of Pt area
- Current probes attached to the pads at the ends of the row
- Voltage probes attached to the pads of device #2 (1,2 in matrix index notation) as these were easiest to wire bond to

---
Top row measurements (test)
- 1231_1427_wo3196_r13
- Two wire resistance measurements (voltage sourced)
- No H2
Temperature setpoint is 25 C
Sample rate is 1 Hz
Measurement time is 60 s
Source voltage is 1.0 V
Limit current starts at 1.5e-08 A
Mean resistance is 7.027011e+07
with std 7.027047e+07

---
Top row measurements (5 min)
1231_1431_wo3196_r13

---
Top row measurements (5 min)
1231_1431_wo3196_r13

---
Top row measurements (10 Hz)
1231_1439_wo3196_r13

---
Device #2
4