## Slide 1: WO3196 IV-curve kinks
Measurements of Device 2 on WO3196
  Light
  Dark
    25 C
    65 C
  In 0.1% H2/Ar at 1 bar
Settings
Max voltage set to 10V
0.2 s measurement time
4 point resistance measurement
I-
I+
V+
V-
Probe location are given in white
Inside green area is crystalline WO3, outside of it is amorphous WO3 on top of LAO
Inside cyan areas there is 5 nm of Pt

## Slide 2: Terms
Light and dark: With and without a window in the chamber
‘Top’, ‘middle’, ‘bottom’ and ‘all’ for IV curve fits:
  Top: Positive voltage part after kink
  Middle: In between kinks
  Bottom: Negative voltage before kink
  All: Entire curve
‘Plus’ and ‘minus’ for IV curves
  Plus: IV curve measured with increasing current
  Minus: IV curve measured with decreasing current
  Minus is measured directly after plus

## Slide 3: Light (with window)
Kinks at 1.5E-7 A and 1.5 V
Name | Measurement | Direction | Position | R (Ohm) | R Std (Ohm)
0117_1703_WO3196_full_IV_curve | Light 25 | Minus | Bottom | 2.29E+07 | 1.48E+05
0117_1703_WO3196_full_IV_curve | Light 25 | Minus | Middle | 1.02E+07 | 5.69E+03
0117_1703_WO3196_full_IV_curve | Light 25 | Minus | Top | 2.35E+07 | 4.31E+04
0117_1703_WO3196_full_IV_curve | Light 25 | Plus | Bottom | 2.15E+07 | 1.09E+05
0117_1703_WO3196_full_IV_curve | Light 25 | Plus | Middle | 1.02E+07 | 1.99E+04
0117_1703_WO3196_full_IV_curve | Light 25 | Plus | Top | 2.39E+07 | 1.53E+05
Fit results

## Slide 4: Dark 25 C
Name | Measurement | Direction | Position | R (Ohm) | R Std (Ohm)
0124_1816_WO3196_full_IV_curve_dark | Dark 25 | Minus | Bottom | 8.05E+07 | 2.78E+04
0124_1816_WO3196_full_IV_curve_dark | Dark 25 | Minus | Middle | 3.16E+07 | 8.11E+04
0124_1816_WO3196_full_IV_curve_dark | Dark 25 | Minus | Top | 8.19E+07 | 2.46E+04
0124_1816_WO3196_full_IV_curve_dark | Dark 25 | Plus | Bottom | 7.96E+07 | 3.31E+04
0124_1816_WO3196_full_IV_curve_dark | Dark 25 | Plus | Middle | 3.14E+07 | 7.42E+04
0124_1816_WO3196_full_IV_curve_dark | Dark 25 | Plus | Top | 8.21E+07 | 3.58E+04
Also kinks at 1.5 V and 0.5e-7 A
Fit results

## Slide 5: Dark 65 C
No kinks at all
Name | Measurement | Direction | Position | R (Ohm) | R Std (Ohm)
0127_1527_WO3196_full_IV_curve_dark | Dark 65 | Minus | All | 1.35E+07 | 8.73E+03
0127_1527_WO3196_full_IV_curve_dark | Dark 65 | Plus | All | 1.33E+07 | 1.47E+04
Fit results

## Slide 6: H2 Dark
Kink also at 1.5 V
Resistance was changing over time, therefore the plus and minus curves are different
Name | Measurement | Direction | Position | R (Ohm) | R Std (Ohm)
0127_1854_WO3196_full_IV_curve_h2_100nA | H2 25 | Minus | Bottom | 1.04E+08 | 4.19E+05
0127_1854_WO3196_full_IV_curve_h2_100nA | H2 25 | Minus | Middle | 4.55E+07 | 2.65E+05
0127_1854_WO3196_full_IV_curve_h2_100nA | H2 25 | Minus | Top | 9.95E+07 | 8.71E+05
0127_1854_WO3196_full_IV_curve_h2_100nA | H2 25 | Plus | Bottom | 8.67E+07 | 4.57E+05
0127_1854_WO3196_full_IV_curve_h2_100nA | H2 25 | Plus | Middle | 4.08E+07 | 2.89E+05
0127_1854_WO3196_full_IV_curve_h2_100nA | H2 25 | Plus | Top | 1.09E+08 | 7.52E+05
Fit results

## Slide 7: Data
Resistances IV curve light |  |  |  | Top = high voltage, bottom = negative voltage | 
Name | Measurement | Direction | Position | R (Ohm) | R Std (Ohm)
0117_1703_WO3196_full_IV_curve | Light 25 | Plus | Middle | 1.02E+07 | 1.99E+04
0117_1703_WO3196_full_IV_curve | Light 25 | Plus | Top | 2.39E+07 | 1.53E+05
0117_1703_WO3196_full_IV_curve | Light 25 | Plus | Bottom | 2.15E+07 | 1.09E+05
0117_1703_WO3196_full_IV_curve | Light 25 | Minus | Top | 2.35E+07 | 4.31E+04
0117_1703_WO3196_full_IV_curve | Light 25 | Minus | Bottom | 2.29E+07 | 1.48E+05
0117_1703_WO3196_full_IV_curve | Light 25 | Minus | Middle | 1.02E+07 | 5.69E+03
0124_1816_WO3196_full_IV_curve_dark | Dark 25 | Plus | Middle | 3.14E+07 | 7.42E+04
0124_1816_WO3196_full_IV_curve_dark | Dark 25 | Plus | Top | 8.21E+07 | 3.58E+04
0124_1816_WO3196_full_IV_curve_dark | Dark 25 | Plus | Bottom | 7.96E+07 | 3.31E+04
0124_1816_WO3196_full_IV_curve_dark | Dark 25 | Minus | Bottom | 8.05E+07 | 2.78E+04
0124_1816_WO3196_full_IV_curve_dark | Dark 25 | Minus | Middle | 3.16E+07 | 8.11E+04
0124_1816_WO3196_full_IV_curve_dark | Dark 25 | Minus | Top | 8.19E+07 | 2.46E+04
0127_1527_WO3196_full_IV_curve_dark | Dark 65 | Plus | All | 1.33E+07 | 1.47E+04
0127_1527_WO3196_full_IV_curve_dark | Dark 65 | Minus | All | 1.35E+07 | 8.73E+03
0127_1854_WO3196_full_IV_curve_h2_100nA | H2 25 | Plus | Bottom | 8.67E+07 | 4.57E+05
0127_1854_WO3196_full_IV_curve_h2_100nA | H2 25 | Plus | Middle | 4.08E+07 | 2.89E+05
0127_1854_WO3196_full_IV_curve_h2_100nA | H2 25 | Plus | Top | 1.09E+08 | 7.52E+05
0127_1854_WO3196_full_IV_curve_h2_100nA | H2 25 | Minus | Bottom | 1.04E+08 | 4.19E+05
0127_1854_WO3196_full_IV_curve_h2_100nA | H2 25 | Minus | Middle | 4.55E+07 | 2.65E+05
0127_1854_WO3196_full_IV_curve_h2_100nA | H2 25 | Minus | Top | 9.95E+07 | 8.71E+05